PRODUCT SPECIFICATION – QuietZone Acoustic Floor Mat

Section 09 80 00 Acoustical Treatment

Section 09 85 00 Sound transmission Control Materials

Part 1 – GENERAL

  - Summary

- Polyethylene foam acoustic floor mat designed to isolate sound vibrations and impact

noise in flooring applications for improved noise control.  Floor mat is placed between

sub-floor and plywood or gypsum concrete overlayment.

- The floor system shall have a minimum IIC rating of _____and a minimum STC rating

of ____ when tested in accordance with ASTM E-492 and ASTM E-90 at an

accredited Acoustical Laboratory.

  - Related Products

- Section 09 85 00 -QuietZone Acoustic Sealant

- Section 09 85 00 -QuietZone Acoustic Batt Insulation

- Section 09 85 00 -QuietZone Acoustic Wall Framing

- Section 09 77 40 -QuietZone Solserene Fabric Ceiling System

- Section 09 54 00 –QuietZone Acoustyle Wood Ceiling System

  - References

- American Society for Testing and Materials (ASTM)

  - E84 Test Method for Surface Burning Characteristics

Flame Spread -20, Smoke Developed -50

  - D 3575-93, Suffix D @ 25%/50% Compressive Strength Vertical Direction

720/18000 (psf)

  - D 3575-93, Suffix B  Compression Set

19% (81% recovery)

  - C 303  Nominal Density

2.2 (pcf)

  - C 3575-93  Water Absorption

<0.1 (psf)

  - C 518-85  Thermal Resistance R-Value

  - (hr-(ft (squared)) – ((degrees) F) /BTU)

  - Submittals

- Product Data:  Submit Owens Corning product literature, installation instructions and product

samples for specified floor mat.

  - Delivery, Storage and Handling

- Protect floor mat from physical damage.  Comply with manufacturer’s recommendations for

handling, storage and protection during installation

- Label for packaging to include material name, production date and/or product code.

  - Limitations

- Combustible.  This product should not be exposed to open flames or possible ignition sources.

This product must be installed with a thermal barrier toward

the interior of the structure.

Part 2 – PRODUCTS

2.01 Manufacturer

A.  Owens Corning

2.02 QuietZone Acoustic Floor Mat

A.   3/8” Thick in rolls, 4 feet wide by 35 feet long

B.   Packaged in rolls 4 feet long and 16 inches in diameter.

Part 3 – EXECUTION

3.01 Inspection

A.  Examine the areas and conditions under which work of this section will be installed.

Verify that adjacent materials are dry and ready.  Verify that electrical and

mechanical sevices within walls have been inspected and tested.  Verify that project

drawings comply with installation requirements.

B.  Provide written report listing conditions detrimental to the performance of work in

this section.  Do not proceed with installation until unsatisfactory conditions have

been resolved.

3.02 Installation

A.   Comply with manufacturer’s instruction for particular conditions of installation

in each case.

B.   Mat must be laid on a clean, dry and level surface.

C.   Overlayment of exterior, AC grade plywood that is uniform, flat, dry and free of defects. (or)

lightweight gypsum concrete poured per manufacturer’s instructions

D.   No fasteners to connect overlayment to subfloor.  Finished floor assembly to “float” on the

QuietZone Acoustic Floor Mat.

3.04 Material Storage and Protection

A.  Protect floor mat from damage and exposure to sun prior to installation.

END OF SECTION