PRODUCT SPECIFICATION – QuietZone Acoustic Wall Framing

Section 09 80 00 Acoustical Treatment

Section 09 85 00 Sound Transmission Control Materials

Part 1 – GENERAL

  - Summary

- Acoustically engineered lumber for wall framing, designed to break sound vibration paths in noise control applications

in residential, multi-family and commercial buildings.  Maintains nominal wall depths for 2x4 and 2x6 wall construction.

  - Related Products

- Section 09 85 00 -QuietZone Acoustic Sealant

- Section 09 85 00 -QuietZone Acoustic Floor Mat

- Section 09 85 00 -QuietZone Acoustic Batt Insulation

- Section 09 77 40 -QuietZone Solserene Fabric Ceiling System

- Section 09 54 00 –QuietZone Acoustyle Wood Ceiling System

  - Submittals

- Product Data:  Submit Owens Corning product literature, installation instructions, product

data sheet and product samples.

  - Delivery, Storage and Handling

A.  Comply with manufacturer’s recommendations for handling, storage and protection before and during installation

  - Limitations

A.  2x4 QuietZone Acoustic Wall Framing has limited load bearing capabilities and should be used for interior walls only.

B.  2x6 QuietZone Acoustic Wall Framing has load-bearing capabilities similar to standard 2x4 wood framing.

Part 2 – PRODUCT

2.01 Manufacturer

A.  Owens Corning

2.02 QuietZone Acoustic Wall Framing

A.  Manufacturing process.  A fully assembled wood stud consisting of structural Tembec finger-jointed

lumber connected to Selectum® Laminated Veneer Lumber (LVL), using Owens Corning's patented

acoustically resilient metal clips.

B.  Tolerance.  QuietZone Acoustic Wall Framing tolerances are:  Length and depth -1/8”, width -1/16”.

C.  Identification.  QuietZone Acoustic Wall Framing is identified by a stamp indicating the product,

manufacturer’s name and product code.

Part 3 – EXECUTION

3.01 Inspection

A.  Examine the areas and conditions under which work of this section will be installed.

Verify that adjacent materials are dry and ready.  Verify that project drawings

comply with installation requirements.

B.  Provide written report listing conditions detrimental to the performance of work in

this section.  Do not proceed with installation until unsatisfactory conditions have

been resolved.

3.02 Installation

A.  Comply with manufacturer’s instruction for particular conditions of installation.

QuietZone Wall Framing members may be laid out and assembled on the floor/deck

in the conventional manner.

B.  The structural member of the stud is attached flush to the top and bottom plates.  The

resilient member is not attached and extends approximately 1/8” past the top and bottom plates.

The resilient member will face the same direction over the entire wall area.

3.04 Material Storage and Protection

If stored prior to installation, need to be protected from the weather.

END OF SECTION